## Slide 1: Traveling wave, lumped element kinetic inductance parametric amplifier for detector readout
Saptarshi Chaudhuri, Dale Li, Kent Irwin, Clint Bockstiegel, Johannes Hubmayr, Joel Ullom, Michael Vissers, Jiansong Gao
July 20, 2017

## Slide 2: TES, MKID benefit from quantum-limited amplifier
Significant benefits of lower amplifier noise
  MKIDs: improve total noise, esp. dissipation readout
  Microwave SQUIDs: significant noise from HEMT, lower noise floor
State-of-the-art follow-on amplifier: HEMT- TN~2-4 K @ 4-8 GHz
Quantum limit: 48 mK/GHz
  Order of magnitude lower!
Need for broadband, high dynamic range, quantum-limited amplifier
Solution: Traveling Wave Kinetic Inductance Parametric Amplifiers
LNF HEMT- TN~2.1 K

## Slide 3: Principles of traveling-wave parametric amplification
Requirements
Traveling-wave structure, i.e. transmission line
Reactive nonlinearity, e.g. current-dependent kinetic inductance L(I)=L0[1+ (I/I*)2]
Dispersion engineering
  Inhibit pump harmonic growth
  Compensate for nonlinear phase slippage to phase match
Four-wave mixing amplifier
ωp
ωp
ωs
ωi
Pump
Signal
Idler
ωs+ωi=2ωp
Phase match for max gain: ks+ki=2kp

## Slide 4: Background: Dispersion-engineered amplifier with periodically loaded CPW
NbTiN (Ic~mA) used for high dynamic range amplification
Stopbands inhibit harmonics, achieves phase match for max gain
Initial demo in Eom et al., Nature Physics 8, pp. 623-627 (2012)
λper/2
Normalized Power Transmission (dB)
Pump
fper
2fper /3
fper /3
0 5 10 15 20 25 30 35 40
Frequency (GHz)
10.5 11 11.5 12 12.5 13
Frequency (GHz)
0
-100
-200
-300
-400
-500
-600
-700
-800
Dispersion keff-k0 (m-1)
5
4
3
2
1
0
-1
-2
-3
-4
-5
X 10-3
Z0=200 Ω

## Slide 5: Successful amplifier, but problems with yield, gain ripple, and noise
CPW spiral 2m length- most chips failed due to opens/ shorts
Large, dense gain ripple- mismatch with external circuit
Pump power of ~200 μW- on-chip heating, thermal noise
  Noise temperature as low as 1 K- 2x better than any HEMT!
~10 MHz ripple period

## Slide 6: Towards a more practical amplifier: Lumped-element transmission line
Inductor strip/ IDC architecture more compact, robust than CPW
  Better yield expected!
Harmonics naturally inhibited by low-pass cutoff
Easy to get 50 Ω impedance, no tapers needed
  Simpler matching, lower power
C/2
C
C
C
C
L
L
L
L
L
L
L
C
C
C/2
Port 1
Port 2

## Slide 7: Phase matching with lumped- element paramps
Periodic Loading
Lumped element analog of CPW loading
Operate far below cutoff- LC looks distributed
Change capacitance to introduce stopbands, dispersion
NEW!: Resonator Phase Shifter
Periodic resonators act as ideal phase shifters to correct mismatch
Enables phase matching at higher nonlinearities now observed in NbTiN
ωp
ωs
0
(S21)[rad]
ωr
ωi
∆θ

## Slide 8: Amplifier design
Periodic Loading
Design Parameters | Periodic Loading | Resonator Phase Shifter
Pump Frequency | 6 GHz | 6 GHz
Impedance | 50 Ω | 50 Ω
Cutoff Frequency | 318 GHz | 55 GHz
Length | 10 cm (70 wavelengths) | 10 cm (70 wavelengths)
Phase Matching | C reduced 5x: 50 Ω → 111 Ω | 6 resonator blocks
Resonator Phase Shifter
100 mm
Resonator Block
Loadings

## Slide 9: Amplifier design
Periodic Loading
Design Parameters | Periodic Loading | Resonator Phase Shifter
Pump Frequency | 6 GHz | 6 GHz
Impedance | 50 Ω | 50 Ω
Cutoff Frequency | 318 GHz | 55 GHz
Length | 10 cm (70 wavelengths) | 10 cm (70 wavelengths)
Phase Matching | C reduced 5x: 50 Ω → 111 Ω | 6 resonator blocks
Resonator Phase Shifter
100 mm
Resonator Block
Loadings
Much smaller! Exploit higher nonlinearities for more efficient gain.

## Slide 10: Amplifier fabrication and packaging
9 amplifier lines per chip, 8 chips on 6” wafer
2/3 of all lines show good Ic, RF transmission
10 cm
1 cm
Much improved device fabrication yield

## Slide 11: Initial results: 15 dB gain, 10x less length, 3x less power!
≥1 GHz of bandwidth on each side of pump sufficient for many applications
Future resonator versions will have higher Qc phase shifters to match periodic loading bandwidth
Periodic Loading
Resonator Phase Shifter
Pump
Pump

## Slide 12: Close to 50 Ω, but excess mismatch still there
Periodic Loading
Resonator Phase Shifter
Measured 47 Ω device impedance
Mismatch at ports still present- wirebonds to blame?

## Slide 13: Parasitic features now clearly observed
No discernable correspondence to length scales
Likely due to environmental coupling, i.e. to box
Resonator Phase Shifter
Periodic Loading

## Slide 14: Next steps
Noise measurements
  Does 3x lower power help by reducing thermal noise?
Heat-sinking and thermal noise mitigation
  Lower trace width, different materials for lower power?
Improve RF ground + connectorization to reduce ripple/parasitics
  Increase groundplane wirebond density
  Continuous connections to ground possible with new architecture
  Mitigate impedance mismatch from ports
Careful analysis of TES/MKID readout applications

## Slide 15: Important application for parametric amplifiers: Light-field dark matter searches
Trio of posters this week:
  A. Phipps- the DM Radio “grand vision” (PE-15)
  S. Kuenstner- the DM Radio Pathfinder (PA-73)
  S. Chaudhuri- fundamental limits on detection (PE-24)

## Slide 16: Summary
Lumped-element traveling-wave parametric amplifier demonstrated with much smaller length, lower power, and higher fabrication yield
Much more practical amplifier
For details: S. Chaudhuri, D. Li, K.D. Irwin, C. Bockstiegel, J. Hubmayr, J.N. Ullom, M.R. Vissers, and J. Gao, Appl. Phys. Lett. 110, 152601 (2017).